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Specifiers: Click on the ¶ icon in the WORD toolbar to reveal detailed instructions.


***NOTE TO SPECIFIER*** This section is based on products of Pecora Corporation, manufacturer of traffic coatings (07 18 00), water repellants (07 19 00), fluid-applied air/weather barriers (07 25 00, 07 27 00, 07 27 26), joint sealants (07 92 00), and high-performance coatings (09 96 00) located at:

165 Wambold Road

Harleysville, PA 19438

Toll Free: 800-523-6688

Tel: 215-723-6051

Fax: 215-721-0286

Email: techservices@pecora.com

Web: www.pecora.com http://www.pecora.com 

SECTION 09 96 53
ELASTOMERIC COATINGS
GENERAL

SECTION INCLUDES

A. Elastomeric wall coating primer.
REFERENCE STANDARDS

B. ASTM C 794 – Standard Test Method for Adhesion-in-Peel of Elastomeric Joint Sealants

C. ASTM D 4541 – Standard Test Method for Pull-Off Strength of Coatings Using Portable Adhesion Testers

D. ASTM D 3960 – Standard Practice for Determining Volatile Organic Compound (VOC) Content of Paints and Related Coatings
PREINSTALLATION CONFERENCE
E. Convene conference at least two weeks before start of work. Require attendance by Architect, Contractor, installer, traffic coating manufacturer, and installers of related work. Discuss existing conditions, substrate test results, mockups, substrate preparation and application procedures, scheduling and protection of work, and other relevant items
ACTION SUBMITTALS

F. Product Data:  Manufacturer’s technical data and tested physical and performance properties.

INFORMATIONAL SUBMITTALS

G. Manufacturer's Instructions: Include storage and handling requirements; substrate evaluation, preparation, and treatment; and installation of traffic membrane including environmental conditions.

H. Reports:  Adhesion test reports.

I. Applicator’s qualification statement.

J. Maintenance Data: Include procedures for cleaning, stain removal, and repairing surface.

K. Warranties:  Samples of special warranties.

QUALITY ASSURANCE

L. Applicator Qualifications:  Engage installers trained, accepted and as recommended by manufacturer.

PRECONSTRUCTION TESTING

M. Field Adhesion Testing:  Provide mockups [10 to 20 sq. ft. in area] [as shown on Drawings] [_____] for evaluation of primer adhesion to [each type of] substrate to receive new exterior wall coatings. Test primer adhesion using one of the following methods:
1. Peel Adhesion:  Minimum 5 pli when tested in accordance with ASTM C 794
2. Pull-Off Strength:  Minimum 50 psi when tested in accordance with ASTM D 4541.

N. Report adhesion testing results. 
O. Do not use primers that fail to adhere to substrates.
DELIVERY, STORAGE, AND HANDLING

P. Deliver products to project site in unbroken packaging with product identification labeling.

Q. Store primers in original undamaged packaging within temperature and humidity limits recommended by manufacturer; protect materials from direct sunlight.

R. Remove and replace products that cannot be installed within their stated shelf life.
FIELD CONDITIONS

S. Do not apply primer when ambient and substrate temperatures are below 40 degrees F (4 degrees C) or when temperatures are expected to fall below 40 degrees F (4 degrees C) within 24 hours after application.
T. Do not apply primer in snow, rain, fog or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 degrees F (minus 15 degrees C) above the dew point; to damp or wet surfaces; or when rain is expected within 24 hours after application.
WARRANTY

U. Material Warranty:  Provide manufacturer’s standard 10-year limited material warranty commencing at date of Substantial Completion. Complete forms in Owner’s name and register with manufacturer.
PART 2 -  PRODUCTS

MANUFACTURERS

A. Pecora Corporation, Harleysville, PA 19438; Tel: 800-523-6688; Fax: 215-721-0286; Web: http://www.pecora.com
1. Substitutions:  Not permitted, no known equivalent.

HIGH PERFORMANCE COATINGS

B. Material Compatibility:  Provide primer that is compatible with existing substrate and new wall coatings and sealants.
PRIMERS

***NOTE TO SPECIFIER*** Pecora SilcoPrime is a unique product in the marketplace with no known comparable equivalents.
C. Primer for Silicone Wall Coating Substrates:  Pecora SilcoPrime.
1. Description:  Silyl-terminated Polyurethane (STPU) interlaminary primer.
2. Application:  Adhering architectural wall coatings to existing exterior silicone coatings applied to concrete, masonry, EIFS (exterior insulation and finish system) substrates, and Portland cement plaster (stucco) substrates.
3. VOC Content:  Less than 98 g/L per ASTM D 3960.
4. Color:  White.

PART 3 -  EXECUTION

EXAMINATION

A. Examine substrates to receive coatings for compliance with elastomeric wall coating manufacturer’s requirements.

B. Verify that surfaces are clean, dry, and free of dirt and other substances that could adversely affect adhesive bond.

C. Do not proceed with application until unsatisfactory conditions have been corrected.

PREPARATION

D. Prepare substrates per manufacturer’s instructions.

E. Using workers skilled in the trades involved, remove hardware, light fixtures, prefinished and similar items.  If removal is impractical or impossible, provide surface-applied protection.
1. When wall coatings have cured reinstall removed items. Remove surface-applied protection, if any.

F. Pressure clean wall surfaces to remove atmospheric, biologic, and other contamination. Prevent damage to existing substrates. Allow cleaned areas to dry before priming.

G. Protect adjoining work from overspray.

1. Mask sealant bond surfaces if coating application precedes sealant installation.

2. Cover aluminum and glass surfaces.

3. Cover vegetation with drop cloths.

APPLICATION
H. Apply coatings to prepared wall surfaces in accordance with manufacturer's instructions.
I. Apply primer at rate to 300 to 500 sq. ft per gallon using brush, roller, or airless sprayer to achieve 3 to 5 wet mil coverage.
J. Apply exterior wall coatings within 72 hours of primer application. Do not leave primed areas exposed to weather greater than 14 days.
CLEANING AND PROTECTION
K. Remove primer from wall surfaces that are not to receive new coatings.

L. Protect primed surfaces from rain, contamination, and damage until new wall coatings are applied.
M. Clean and repair damaged surfaces per primer manufacturer’s recommendations.

N. Before application of wall coatings, test primed surfaces that have been cleaned and repaired for adequate adhesion of subsequent coats. Reprime areas where coatings fail to adhere.
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